## Slide 1: Helium bubble density sample 21BT
Aix en Provence 26.02.2021
Mykola Ialovega
CEA Cadarache, IRFM
Université d’Aix Marseille, PIIM laboratory
Supervisors: E. Bernard1, R. Bisson2, C. Grisolia1
Thesis Director: T. Angot2
IRFM, SI2P, CEA/Cadarache
Université d’Aix Marseille, PIIM

## Slide 2
Experimental protocol

## Slide 3
HF after Helium irradiation
SURFACE (SEM):
Oval-shaped holes
white W particles
undulating surface structure on (111) that is aligned with <100> direction
HF:

## Slide 4
HF after Helium irradiation
NEAR SURFACE (TEM):
Holes are open bubbles
Bubbles not shaped:
small d<3 nm
middle 3<d<10 nm
large d>10 nm
Many small bubbles close to the surface; up to 40-50 nm below the surface
HF:

## Slide 5
HF after Helium irradiation: bubbles density
When I do the analysis of the TEM data, the main assumptions are:
Bubbles are spherical: Diameter is recalculated using the area of each bubble However, not all the bubbles are spherical!
In-depth position of each bubble is the distance between the interception point of major and minor radius of the bubble and the surface
The surface is the border line between W (dark contrast) and Pt (brighter contrast) layers (see the previous slide)

## Slide 6
HF after Helium irradiation: bubbles density
How many bubbles we cross when we cut the lamella parallel to the sample’s surface (so, density in depth)
Bubbles number vs diameter
All bubbles analyzed using one lamella (using 12 under focused and corresponding 12 over focused TEM images):
Max number of so-called
middle-size bubbles (3-5 nm in diameter)
Max number of bubbles at a depth of ~10 nm below the surface
Bubbles burst when their diameter>distance to the center of the bubble
Note:
The calculation gives good results for bubbles with d>=3nm up to the depth of ~30-40nm